Impact of redox conditions on the binding of redox-inert contaminants to magnetite

Rémi Marsac1, Laura Fablet2,3,4, Jaimy Scaria2, Mathieu Pédrot2, Fadi Choueikani3

1 Université Paris Cité, Institut de physique du globe de Paris, CNRS, F-75005 Paris, France

2 Univ Rennes, CNRS, Géosciences Rennes – UMR 6118, F-35000 Rennes, France.

3 Synchrotron SOLEIL, L'Orme des Merisiers, Saint- Aubin BP48, 91192 Gif-sur- Yvette cedex.

4 BRGM.

Magnetite nanoparticles (MNs, FeIIFeIII2O4) play an important role on the behavior and fate of many contaminants and are widely used in environmental applications due to their small size, high surface area, redox and magnetic properties. Structural Fe(II) in stoichiometric MNs (R = [Fe(II)]/[Fe(III)] = 0.5) is extremely sensitive to oxidation, proton and ligand-promoted dissolution, leading to the formation of non-stoichiometric magnetite (0 <  R < 0.5) or maghemite (R = 0; FeIII2O3).1 MNs stoichiometry can then be restored with Fe(II) or chemical reductants, which makes their structure highly dynamic in fluctuating redox environments.

The effect of redox conditions (or magnetite stoichiometry) on the reduction processes of various contaminants (e.g. U(VI), Cr(VI), organics) have been studied carefully.2 However, most of the sorption experiments with redox-inert elements were carried out in O2 atmosphere, using NO3- as background electrolyte or at acidic pH. Therefore, the impact of R on the binding of redox-inert contaminants to magnetite has been overlooked, although its ability to bind ions and molecules may heavily rely on R, as evidence for silicate, humic acid and quinolone antibiotics.3

Here we summarize our results on the interaction of Co(II),4 Ni(II),5 and Cr(III)6 (considered redox-inert in reduced environments) with magnetite for various stoichiometries (0.1 ≤ R ≤ 0.5). Surface speciation of metal ions (M) was probed by X-ray absorption spectroscopy (XAS) and/or X-ray magnetic circular dichroism (XMCD) at Co/Ni L2,3-edges on DEIMOS, XAS at Cr K-edge on LUCIA, and HERFD-XAS at Ni K-edge on FAME-UHD. Stoichiometric magnetite (R0.5) incorporates metal ions in its structure at low [M] (as MFe2O4-like phases), whereas surface complexes form on quasi-maghemite (R0.1). At high [M], R0.5 surface was a better template for M-hydroxide surface precipitation than R0.1. These results highlight the necessity to carefully preserve, control or monitor magnetite stoichiometry and will help to predict the effect of magnetite on metal fate and ecotoxicity in the environment.

# References

(1)	Jungcharoen, P.; Pédrot, M.; Heberling, F.; Hanna, K.; Choueikani, F.; Catrouillet, C.; Dia, A.; Marsac, R. Prediction of Nanomagnetite Stoichiometry (Fe(II)/Fe(III)) under Contrasting pH and Redox Conditions. Environ. Sci.: Nano 2022, 9 (7), 2363–2371. https://doi.org/10.1039/D2EN00112H.

(2)	Latta, D. E.; Gorski, C. A.; Boyanov, M. I.; O’Loughlin, E. J.; Kemner, K. M.; Scherer, M. M. Influence of Magnetite Stoichiometry on UVI Reduction. Environ. Sci. Technol. 2012, 46 (2), 778–786. https://doi.org/10.1021/es2024912.

(3)	Cheng, W.; Marsac, R.; Hanna, K. Influence of Magnetite Stoichiometry on the Binding of Emerging Organic Contaminants. Environ. Sci. Technol. 2018, 52 (2), 467–473. https://doi.org/10.1021/acs.est.7b04849.

(4)	Fablet, L.; Choueikani, F.; Pédrot, M.; Marsac, R. What Are the Effects of Environmental Factors on Co Speciation at the Magnetite Surface? Environ. Sci.: Nano 2024, 11 (5), 2036–2048. https://doi.org/10.1039/D3EN00962A.

(5)	Fablet, L.; Pédrot, M.; Choueikani, F.; Kieffer, I.; Proux, O.; Pierson-Wickmann, A.-C.; Cagniart, V.; Yomogida, T.; Marsac, R. Nickel Binding with Magnetite Nanoparticles. Environ. Sci.: Nano 2025, 12 (5), 2815–2827. https://doi.org/10.1039/D4EN01114G.

(6)	Scaria, J.; Pédrot, M.; Fablet, L.; Yomogida, T.; Nguyen, T. T.; Sivry, Y.; Catrouillet, C.; Pradas Del Real, A. E.; Choueikani, F.; Vantelon, D.; Dia, A.; Groleau, A.; Marsac, R. Magnetite Stoichiometry (Fe(II)/Fe(III)) Controls on Trivalent Chromium Surface Speciation. Environ. Sci. Technol. 2025, 59 (11), 5747–5755. https://doi.org/10.1021/acs.est.4c12899.