Multiple-Edge EXAFS/RMC Refinement for 3D Local Structure in SrTiO3

Kai Kamijo1, Nobuo Nakajima1, Dongxiao Fan2 and Andris Anspoks3 (presenting author)

1 Graduate School of Advanced Science and Engineering, Hiroshima University, 1-3-1 Kagamiyama, Higashi-Hiroshima 739-8526, Japan
2 Institute of Materials Structure Science, High Energy Accelerator Research Organization (KEK), 1-1 Oho, Tsukuba, Ibaraki 305-0801, Japan
3 Institute of Solid State Physics, University of Latvia, Kengaraga Street 8, Riga LV-1063, Latvia

ABSTRACT

Conventional EXAFS analysis is still often performed edge by edge, although many functional materials contain several absorber atoms whose local environments are strongly coupled. A single-edge fit can reproduce an EXAFS spectrum while leaving correlated distances, disorder factors, multiple-scattering contributions and light-element positions underdetermined. We present a practical multiple-edge strategy in which Sr-K and Ti-K edge EXAFS spectra of SrTiO3 are fitted simultaneously to one reverse Monte Carlo (RMC) structural model [1-4]. The aim of this presentation is methodological: to show how two absorption edges provide complementary constraints that make the local oxygen geometry and angular distortions observable within standard hard X-ray EXAFS. It also aims to facilitate use of RMC for EXAFS analysis as RMC remains underused in routine EXAFS analysis, especially as a complement to conventional shell fitting.

Transmission spectra of SrTiO3 collected from 26 to 300 K were analyzed with EvAX using a 6×6×6 tetragonal supercell (4320 atoms), multiple scattering paths, and Morlet wavelet-transform comparison [2].

The SrTiO3 benchmark illustrates why multiple-edge modelling matters. Earlier single-edge RMC analyses could not resolve the antiphase TiO6 octahedral rotation, whereas simultaneous Sr-K/Ti-K refinement recovers radial distribution functions, MSRDs, Voronoi volumes, and oxygen-position distributions from one consistent 3D model [1]. The local model shows rigid Ti-O bonding, softer Sr dynamics and an in-plane TiO6 rotation reaching 2.7° at 26 K. This approach also builds on one of the early two-edge EXAFS/RMC-EA demonstrations in MnWO4 and Mn0.7Co0.3WO4 [4,6]. Multiple-edge EXAFS/RMC therefore offers the XAS community a robust and practical route from spectra to three-dimensional local structure.

REFERENCES

1.  K. Kamijo, N. Nakajima, D. Fan and A. Anspoks, J. Synchrotron Rad. 32, 1010-1016 (2025).

2.  J. Timoshenko, A. Kuzmin and J. Purans, Comput. Phys. Commun. 183, 1237-1245 (2012).

3.  A. Anspoks, J. Timoshenko, D. Bocharov, J. Purans, F. Rocca, A. Sarakovskis, V. Trepakov, A. Dejneka and M. Itoh, Ferroelectrics 485, 42-52 (2015).

4.  J. Timoshenko, A. Anspoks, A. Kalinko, I. Jonane and A. Kuzmin, Ferroelectrics 483, 68-74 (2015).

5.  A. Di Cicco and A. Trapananti, J. Phys. Condens. Matter 17, S135-S144 (2005).

6. F. Iesari, R. Osone, S. Kasai, K. Yasukawa, Journal of the Physical Society of Japan 95, 044602 (2026)