Copper Dynamics beyond Lone-Pair Chemistry: A Bonding-Driven Route to Strong Anharmonicity and Low Thermal Conductivity

Animesh Bhui, Emmanuel Guilmeau

CRISMAT, CNRS, Normandie Univ., ENSICAEN, UNICAEN, Caen 14000, France

Abstract. Stereochemically active lone pairs are widely invoked as a chemical design principle for inducing strong anharmonicity and suppressing lattice thermal conductivity in crystalline solids. Here, we identify a complementary mechanism in which localized copper dynamics, rather than lone-pair activity, dominate the lattice response. Cu3Bi2S4Cl provides an ideal platform to disentangle these effects because its crystalline framework simultaneously contains distinct Cu coordination environments and stereochemically active Bi3+ lone pairs. Despite its well-ordered crystal structure, Cu3Bi2S4Cl exhibits glass-like thermal transport, with a lattice thermal conductivity of  0.24 W m1 K1 at 473 K. Temperature-dependent single-crystal diffraction and total-scattering measurements reveal highly anisotropic and site-selective Cu displacements, with Cu(3) exhibiting pronounced off-centering and a broad distribution of local Cu–S environments. Bonding analysis further identifies weak Cu–S interactions within a hierarchical bonding network, providing a soft potential landscape for Cu motion. Crucially, inelastic neutron scattering and anharmonic phonon calculations reveal strongly temperature-dependent, low-energy (<2 THz) vibrational modes dominated by Cu, accompanied by pronounced anharmonic renormalization. These localized Cu dynamics strongly modify phonon transport and drive the system toward a phonon-glass regime, while the contribution of the Bi3+ lone pair is comparatively modest. In this poster, I will present how these findings establish localized Cu dynamics, enabled by coordination and bonding heterogeneity, as a complementary design principle to lone-pair chemistry for engineering strongly anharmonic solids with ultralow thermal conductivity.