Incommensurate Structural Modulation as a New route toward Strong Phonon Scattering in Cu-Sn-Se Chalcogenides

Mia-Eussa Gautier1*, Animesh Bhui1, Pierric Lemoine2, Carmelo Prestipino1, Bin Zhang3, Xioayuan Zhou3, Susumu Fujii4, Julien Varignon1, Philippe Boullay1, Emmanuel Guilmeau1*

1 Laboratoire de cristallographie et Sciences des Matériaux, Université de Caen Normandie, ENSICAEN, CNRS, Normandie Univ, CRISMAT UMR6508, F-14000 Caen, France

2 Institut Jean Lamour, UMR 7198 CNRS – Université de Lorraine, 54011 Nancy, France

3 College of Physics and Institute of Advanced Interdisciplinary Studies, Chongqing University, Chongqing 401331, China

4 Division of Materials and Manufacturing Science, Graduate School of Engineering, Osaka University, Suita, Osaka 565-0871, Japan – Department of Materials, Faculty of Engineering, Kyushu University, Motooka, Fukuoka 819-0395, Japan

*Emails: mia-eussa.gautier@ensicaen.fr ; emmanuel.guilmeau@ensicaen.fr

In recent years, copper-rich sulfides and selenides have attracted increased interest as thermoelectric materials due to their low-cost and environmentally benign nature, as compared to state of art tellurides. Within the Cu-Sn-Q (Q= S; Se) phase diagram, several compounds have been reported, including Cu2SnS3, Cu22Sn10S32, Cu5Sn2S7, Cu4SnS4, Cu2SnSe3, Cu5Sn2Se7 exhibiting promising thermoelectric properties [1],[2] . Variations in the Cu/Sn ratio give rise to different cationic ordering and crystal structures, often derived from the sphalerite-type structure, and lead to diverse electrical and thermal transport behaviors. However, the Cu-Sn-Se crystal structures remains poorly investigated and understood, with compounds displaying a high sensitivity to synthesis conditions and composition, therefore offering an opportunity to unravel new structure types and new mechanisms for electrical conduction and phonon suppression [3].

By using advanced structural characterization techniques, such as 3D electron diffraction (3D ED) and HAADF-STEM analyses, we have elucidated the complex crystal structure of a new compound in the Cu-Sn-Se system. Exhibiting an original crystal arrangement characterized by an incommensurately occupation modulation, this new phase is the first incommensurate structure in the Cu-Sn-Se system. This unusual arrangement has shown to directly impact the thermal transport properties, therefore suppressing the lattice thermal conductivity through strong phonon scattering. These results establish incommensurate modulation as a previously unexplored mechanism for controlling charge and phonon transport in Cu–Sn–Se compounds and highlight structural modulation as a promising crystal-chemistry strategy for designing low-thermal-conductivity thermoelectric materials.

[1] Kumar, V. P. et al, Inorg. Chem. 2021, 60 (21), 16273–16285 and references therein

[2] Fan, J. et al, Inorg. Chem. 2013, 52 (19), 11067–11074 and references therein

[3] Fan, J. et al, Dalton Trans. 2014, 43 (44), 16788–16794 and references therein