CLSF-2026  Poster,  Agnese Primieri 
Composite phases with translational disorder
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The MCr₂X₄ family (M = Pb, Sr, Ba, Eu, Sn; X = S, Se) comprises structurally complex compounds characterized by incommensurate channel-type frameworks [1]. Their structures are based on a hexagonal network of edge-sharing CrX₆ octahedra that defines two distinct types of channels: one hexagonal channel per unit cell, occupied by M₆Cr₂X₆ units, and two trigonal channels containing columns with an approximate M₃X composition. The periodicity of these guest columns may differ from that of the host framework, giving rise to structural incommensurability and, in some members of the family, significant translational disorder. Previous electron diffraction studies of BaCr₂Se₄ [2] and SnCr₂S₄ [3] have demonstrated different types of ordering and disorder within the channels. Such structural complexity is expected to influence charge and thermal transport, making these compounds of interest for thermoelectric applications [3].
In this work, PbCr₂S₄ was investigated as a model system, followed by partial substitution of Cr by V to form PbCr₂₋ₓVₓS₄ (x = 0.4, 0.6, 0.8, and 1). The substitution strategy was motivated by the metallic conductivity previously reported for SrV₂S₄ by Omloo et al. [1], with the aim of exploring whether V incorporation could modify the electronic properties of PbCr₂S₄. The compounds were synthesized by high-temperature solid-state reactions from stoichiometric amounts of high-purity elements sealed in evacuated silica tubes. For V-containing compositions, the silica tubes were carbonized to prevent reaction between V and the silica.
Pure PbCr₂S₄ was successfully obtained. Electron diffraction measurements reveal that coherence between the guest columns is maintained for specific values of l, indicating a degree of ordering within the channels. This behavior differs from that reported for BaCr₂Se₄, where the guest columns exhibit a larger periodicity, and SnCr₂S₄, where the columns are reported to be completely disordered. In the PbCr₂₋ₓVₓS₄ series, compositions with x = 0.4, 0.6, and 0.8 were obtained with minor binary sulfide impurities, while the x = 1 composition contained significant amounts of PbS and Cr₂S₃. Attempts to synthesize the fully substituted PbV₂S₄ phase were unsuccessful.
Powder X-ray diffraction reveals a systematic evolution of the lattice parameters with increasing V content, consistent with progressive V incorporation into the structure. TEM-EDX further confirms the presence of V, although its spatial resolution is insufficient to determine the specific crystallographic sites occupied by the substituting atoms. 
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